Sorption of vanadium on artificial phosphates depending on the concentration

Кайратова А.О., Нурмуханбетова Н.Н.

Магистрант 2 курса

НАО «Кокшетауский университет имени Ш.Уалиханова»,

факультет естественных наук, Кокшетау, Казахстан

E-mail: araika.dosmaganbetova@gmail.com

The teachers of the department decided to use natural phosphates of apatite and phosphorite as sorbents of vanadate ions, as well as to increase the amount of artificial phosphates, to study the presence of vanadium in sediment and superphosphate. In this case, calcium apatite ions can be converted into ions of other divalent metals, and phosphorus ions in the fluorapatite molecule can be converted into ions of various acids. In addition, as a result of chemical reactions between phosphate and vanadium, complex compounds can be formed. According to the above, we determined that of the two studied artificial phosphates, Table 1 and Figure 1: vanadium is better sorbed on superphosphate. Thus, from dilute solutions with a concentration of 0.288 g/l, vanadium is sorbed up to 63 %.

Table 1. Influence of vanadium concentration on its sorption by artificial phosphates / static conditions /, sample 20 g, solution volume 100 ml.

| N | Concentration of V in the initial solution in g/l | рН | Precipitate | рН | Superphosphate |
| --- | --- | --- | --- | --- | --- |
|  |  | initial | equilib. | exchange capacity in mg/g | % sorption of V from solution | initial | equilib. | exchange capacity in mg/g | % sorption of V from solution |
| 1 | 1.19 | 6.57 | 6.74 | 0.695 | 11.8 | 6.57 | 4.15 | 1.12 | 18.9 |
| 2 | 0.586 | 6.50 | 6.70 | 0.675 | 23.2 | 6.50 | 4.09 | 1.1 | 37.9 |
| 3 | 0.288 | 6.31 | 6.31 | 0.425 | 32.0 | 6.31 | 3.96 | 0.82 | 63.0 |

Apparently, superphosphate exhibits some observation in relation to vanadium in connection with the chemical interaction with the formation of calcium vanadates or heteropolycompounds with the general formula H7[P(V3O9)4].

As the concentration decreases, the % extraction of vanadium from the solution increases from 18.9 % to 63 %. At low concentrations6 corresponding to 0.288 g/l, the sorption of vanadium on superphosphate is 0.82 mg/g, which is close to its sorption on sulfonated coals. The pH of the equilibrium solutions is higher than the initial one, which is obviously due to the partial interaction of acid solutions of vanadate with phosphate minerals.

Taking into account the slight difference in the values of the exchange capacity, it was decided to carry out experiments under dynamic conditions on superphosphate, since the latter has a greater porosity than the precipitate, which improves the filtration of the solution through the sorbent layer.

Letters

1. Редкие и рассеянные элементы. Химия и технология. В 3-х книгах. Книга II: Учебник для вузов / Коровин С.С., Дробот Д.В., Федоров П.И./ Под ред. С.С. Коровина. М.: МИСиС, 1999.-С.- 464-480

2. Способы извлечения ванадия из ванадийсодержащего сырья / А.Е.Чурилов, Е.Г.Мукаев, А.В.Горбунова, А.Я.Сучкова // Успехи современной науки и образования. 2016. № 12. Т.5. С. 162-164.

3. Шубина М.В., Махоткина Е.С. Гидрометаллургический способ извлечения ванадия из шлака // Актуальные вопросы химической технологии и защиты окружающей среды: сборник материалов III Всероссийской конференции с международным участием / отв. ред. К.В. Ли- пин. Чебоксары: Изд-во «Новое время», 2013. С. 151- 152.

4. X.W. Wang and M.Y. Wang. A technology for producing V2O5 product from containing vanadium/ Chine patent 201110262556.4, 2011.